SOLID STATE MICROELECTRODE MATERIALS

Working Electrode Fabrication Materials

1)	4 or 5 mm borosilicate glass tubing drawn to a pasteur pipette style tip for sediment profiling & biofilm applications, or PEEK HPLC tubing for water column work.

2)	small tipped burner for drawing glass

3)	BNC cable (from Newark Electronics)

Belden 8216-100-10; RG-174U/type 50 ohm coax cable (0.095 in diameter)

4)	 BNC connectors (from Newark Elehctronics)

Amphenol Corp. #999-226B (Newark Electronics 40F6325) 69745 description

use Ag solder to solder Cu conducting wire of BNC to the BNC connector

Underwater connectors - RMA-SL-FS (Impulse)

5)	a) silver solder - need a soldering iron to melt the solder and connect the BNC cable to the Au wire

OR

b) silver epoxy to make connection between BNC cable and gold (or other metal) sealed in glass (we don=t use this any more)

EPO-TEK Ag epoxy # H2O-E from Epoxy Technology, Inc.

2 parts needed; part A and part B

- We take the cable from 5a and place it into the drawn glass from 1.  A clear epoxy is then used to fill the glass and secure the cable in the glass.  We’ve tried several clear epoxies with success.  The one we use most is West Marine 105 epoxy with 206 hardener in 5:1 ratio.

- After sealing/curing, the tip of the electrode is then sanded until the gold wire is readily observed.  Then 4 different polishes are used to give a clean surface.  Each polish is used for 30-60 seconds in decreasing size.  After polishing, the electrode is plated with Hg and polarized (see below).

Polishes from Buehler -  Working Electrode Materials

Metadi polish			#40-6212	15 Micron

Metadi polish			#40-6172	 6 Micron

Metadi polish			#40-6132	 1 Micron

Metadi polish			#40-6112	0.25 Micron

Metadi  Fluid			#40-6014	(4 oz.)

Buehler Polishing Cloth	#40-7216	(1, 0.25 Micron polish)	(Microcloth)

Buehler Polishing Cloth	#40-7618	(15, 6 Micron polish)	(Texmet)

Double Sticky Tape

240 and 400 Grit Sand paper to sand tips for glass removal after glassblowing gold into glass

Polishers for working electrodes

1)	Simple Polisher - Homemade

9-18 V DC motor mounted on a rack (wood or metal); Aluminum stubs mounted on motor shaft (use Allen Screws); connect motor to 12 V power supply (Radio Shack Micronta 22-127 D); 12 V power supply is regulated by a VARIAC transformer

2)	and/or Narishige model EG-40 or similar

Micromanipulators (several to choose from)

1)	Narishige MN-153

2)	Narishige M-3333

3)	Narishige MO-150		fine scale control to 2 micrometer

4)	Kite from World Precision Instruments #64225

with M10- magnetic base for any of these

Or use old microscope stages that can be adapted

Hg Plating Solution

3.4 g Hg(NO3)2 in 100 mL H2O containing about 300 microliters of concentrated HNO3.  Purge the solution with ultra-pure Ar or N2 gas and then plate at -0.1 volt for 4 min. Add more HNO3 if the Hg(II) begins to precipitate.

Polarization Materials

1)	1N NaOH in small beaker

2 )	9V battery

3)	Pt wire goes to pos lead of 9V battery

4)	Au/Hg electrode goes to neg lead of 9V battery

5)	Polarize for 90sec.

Other Electrodes

1)	reference - SCE or Ag/AgCl

salt bridge recommended for reference

2)	counter electrode - Pt

3)	Vicor frits for references and salt bridge; agarose (5-10% prepared) can be used for the salt bridge instead of frits.

Microscope

1)	Need 100X – Radio Shack is OK.  Can be handheld variety but easier if clamped for stability.

2)	Build a holder for working electrode to check tip.

3)	PowerMax sells a computer USB controlled one from Bodelin called ProScope. SCA-127387

Miscellaneous items

1)	Faraday cage

2)	electrochemical cells

3)	BNC cables

4)	electrical equipment - Ag solder, soldering iron, voltmeter, heat shrink tubing (3/16 BK 3473 from Newark Electronics)

5)	assorted clamps, ring stands

6)	Ultrasonic cleaner and cleaning solution (Buehler #75-5000-032 diluted 20:1 in distilled water)

- Underwater electrical materials - the top end of the electrode can be coated with 2 applications of Scothkote (3M) electrical coating and Scothfil (3M) electrical insulation putty which makes a water proof seal. Use Scotch Super 33 electrical tape for final wrapping.

Buehler

41 Waukegan Road

Lake Bluff, IL 60044 U.S.A.

800-buehler

708-295-6500

Epoxy Technology, Inc.

14 Fortune Drive

Billerica, MA 01821 U.S.A.

508-667-3805

Newark Electronics

7272 Park Circle Drive

Hanover, MD U.S.A.

410-712-6922

Optical Appartus Co., Inc.			World Precision Instruments, Inc.

distributor for Narischige			175 Sarasota Center Boulevard

136 Coulter Avenue				Sarasota FL  34240-9258

P.O. Box 352					941-371-1003

Ardmore, PA 19003-0352 U.S.A.

pH microelectrodes

MI-410 combination electrode from

Microelectrodes, Inc.

298 Rockingham RD

Londonderry, NH 03053

1 mm metal enclosed tip combination electrode from

Diamond General

3810 Varsity Drive

Ann Arbor, MI 48108

313-973-7160

Underwater connectors

Impulse

8254 Ronson Road

San Diego, CA 92111

800-327-0971

RMA-SL-MP/ 0.95 w /contact (outer)

RMA-SL-FS/ 0.95 w /contact (inner)

RMA-FSD HP – dead ends

precious metal wires (Premion grade for Au)

Alfa Aesar

800-343-0660

30 Bond St.

Ward Hill, MA 01835-8099

Microscope – computer controlled

PowerMax sells a Bodelin product

6077A Lakeview Blvd.

Lake Oswego OR  97035

1-800-441-6877 or 503-624-1827